УДК 517.498:519.6:536.12:621:891

Математичне моделювання і експериментальне дослідження

температури спалахів / Ю. І. Ковальчик // Вісник Харк. нац. ун-ту., – 2008. –

№ 833. Сер. «Математичне моделювання. Інформаційні технології.

Автоматизовані системи управління», вип. 10. – С. 140-148 : мал. 1. - табл. 1.

– Бібліогр.: 12 назв.

Актуальною теоретичною і прикладною проблемою є визначення

максимальних температур, які виникають на мікроконтакті в процесі сухого

тертя без мащення. Зроблений короткий аналіз існуючих моделей температури

спалахів. Проаналізовані межі їх застосування. Запропоновані нові модифікації

цих моделей і їх розв’язки із застосуванням нового математичного апарату

континуального інтегрування. На основі модифікації моделі А.В.Чічінадзе

здійснені розрахунки максимальної температури за навантаження Р=1.5N і

швидкості 0.1m/s.Наведені дані експерименту щодо визначення величини

спалахів температури для пари тертя хромель-алюмель. Показано, що дані

теоретичних розрахунків і експерименту добре корелюють між собою.

UDC 517.498:519.6:536.12:621:891

Mathematical modelling and experimental research of the flash temperature /

Kovalchyk Yu. I. // Bulletin of V. Karazin Kharkiv National University, – 2008. –

№ 833. Series «Mathematical Modelling. Information Teghnology. Automated

Control Systems», Issue 10. – P.140-148: Pic. 1. – Tabl. 1. - Ref.: 12 titles

(In Russian)

The actual theoretical and applied problem is the determination of maximal

temperature what occur on the microcontact in the process of dry friction without

lubrication. The short analysis of existing models temperature flashes have been made.

The boundaries of its applying have been shown. The new modifications of this

mathematical apparatus of continual integrating have been proposed.The maximal

temperature at the load 1.5N and speed 0.1m/s has been calculated on the base of

model A.V. Chichinadze modification. Experimental results for flash temperature of

friction pair chromel-alumel has been represented. The good correlation of theoretical

and experimental results has been acquired.

Keywords: friction, flash temperature, continual integrating, thermopair chromelalumel.